MIX OPTIMIZATION FEASIBILITY

Cross-Validated Results from Available IMTS Batch Data

Five-fold GroupKFold validation by projectId | 13,133 strength-eligible records

KEY RESULT Batch data has meaningful predictive value, but current error levels support historical performance screening and engineer review—not fully automated mix optimization.

## Validated model performance

| Analysis | Best model | Records | Mean R² | R² range | MAE (psi) | RMSE (psi) |
| --- | --- | --- | --- | --- | --- | --- |
| Batch-only design-time | ExtraTrees | 13,133 | 0.405 | 0.263–0.520 | 545 | 811 |
| Field-adjusted quality | ExtraTrees | 11,735 | 0.396 | 0.263–0.449 | 509 | 741 |

Interpretation: Single-split R² values of 0.18 and 0.45 reflected project selection. Cross-validation places expected batch-only performance near R²=0.40, with meaningful variability across projects.

## What the results mean

Predictive value. ExtraTrees reduced MAE by approximately 221 psi versus the DummyMedian baseline (766 to 545 psi), demonstrating useful signal in the available batch records.

Field measurements. On identical complete-case folds, adding actual slump and air improved mean R² by about 0.04 and reduced MAE by about 19 psi. These measurements support post-placement quality analysis but are unavailable when designing a new mix.

Reliability limit. Batch-only P90 absolute error was approximately 1,092 psi, and R² varied from 0.263 to 0.520. Predictions therefore require conservative margins and engineering review.

## Recommended use and next step

Use now. Rank existing supplier–plant–mix combinations by historical strength, variability, failure rate, cementitious content, and specification margin; flag review candidates for a materials engineer.

Do not automate yet. Do not automatically reduce cement, approve new proportions, or claim carbon optimization from the current model alone.

Data needed for optimization. Consistent cement and SCM types, admixture product and dosage, aggregate gradation and source, batch water corrections, material cost, and approved product-specific emission factors.