IMTS MIX OPTIMIZATION ANALYSIS

Best Use of Available IMTS Data

A practical path from historical batch records to materials-engineer review

RECOMMENDATION Use IMTS to screen proven historical mixes and identify engineering-review candidates. Current data does not support fully automated mix redesign or cement reduction.

## Evidence from the machine-learning test

| Model scope | Best model | Records | Mean R² | R² range | MAE (psi) | P90 error |
| --- | --- | --- | --- | --- | --- | --- |
| Batch-only strength | ExtraTrees | 13,133 | 0.405 | 0.263–0.520 | 545 | 1,092 psi |

Finding: Batch data contains useful signal, but project-to-project variability and prediction error are too large for automatic optimization.

## Recommended IMTS workflow

| 1 Select office | 2 Keep projects with ≥30 tests | 3 Group by supplier–plant–mix–strength | 4 Calculate risk and performance | 5 Engineer review |
| --- | --- | --- | --- | --- |

## Use case — Project 19225, Los Alamos Transit Mix, Plant 1

| Mix | Review flag | Tests | Avg strength | Failure | Avg margin | P10 margin | Cementitious |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 4K | Quality Risk | 40 | 4,531 psi | 12.5% | +531 psi | −5 psi | 615.7 lb/yd³ |
| 4KI | Optimization Review | 68 | 6,534 psi | 0% | +2,534 psi | +1,996 psi | 616.4 lb/yd³ |

Interpretation. Both mixes used nearly the same cementitious content and the same 4,000-psi requirement, yet 4K had five failures while 4KI had none and exceeded the requirement by more than 2,500 psi on average.

Action. Investigate 4K for production/field issues; review 4KI as a trial-batch optimization candidate. Confirm air requirement, cement/SCM type, admixture dosage, durability requirements, and approved submittal before any change.

BEST CURRENT USE Historical mix screening + transparent review flags + materials-engineer validation. Machine learning is supporting evidence, not the decision maker.