TECHNICAL ASSESSMENT

IMTS Mix Optimization Feasibility and Historical Mix Performance Analysis Plan

Purpose: Evaluate whether current IMTS batch data supports ML-based mix optimization and define a practical next analysis.

Scope: US-unit concrete tests with batch, field-measurement, specification, and specimen-strength data.

Status: Automatic optimization not supported by current model performance; historical mix review recommended.

Decision Do not use the current batch-only strength model to recommend cement reductions or approve new mix designs. Use the data first to identify historically stable, over-performing mixes for engineering review.

# 1. Executive Summary

The current IMTS batch dataset contains measurable relationships with air, slump, and 28-day strength, but it does not support reliable automatic mix optimization. The batch-only strength model achieved only about R² = 0.18, with an MAE of about 662 psi, RMSE near 1,280 psi, and P90 absolute error near 1,135 psi. These errors are too large for safely reducing cement while assuring required strength.

The data remains valuable for a different business use: Historical Mix Performance Analysis. Instead of asking the model to invent or optimize a new recipe, IMTS can group actual historical tests by supplier, plant, mix number, required-strength class, and applicable specifications. It can then quantify strength reliability, failure rate, variability, field compliance, and material use. The output becomes a defensible list of mix-design review candidates for a materials engineer.

# 2. Evidence from the Surrogate Models

| Target | Best model | MAE | RMSE | R² | P90 abs. error | Assessment |
| --- | --- | --- | --- | --- | --- | --- |
| Air (%) | HistGradientBoosting | 0.93 | 1.32 | 0.585 | 2.20 | Moderate signal; not a tight specification guarantee |
| Slump (in) | ExtraTrees | 1.20 | 1.58 | 0.238 | 2.55 | Weak; error can exceed a typical tolerance |
| 28-day strength (psi) | ExtraTrees | 662 | 1,280 | 0.180 | 1,135 | Insufficient for automatic optimization |

The strength model improves over the Dummy median baseline (MAE approximately 858 psi), so the batch fields contain some useful signal. However, the improvement is not strong enough to turn the model into a safe design optimizer. A low global average error would not be sufficient by itself; the high RMSE and P90 error show that some predictions can be wrong by a large amount.

# 3. Why Current IMTS Data Is Not Adequate for ML Mix Optimization

## 3.1 Optimization requires causal recipe information, not only correlation

A predictive model can learn that certain historical recipes were associated with higher strength. Mix optimization asks a harder question: what will happen if one material quantity is deliberately changed while the remaining materials, production process, and curing conditions are controlled? The present IMTS extract is observational. Differences between mixes can also reflect supplier practices, cement source, admixture products, project requirements, weather, testing practices, and other unrecorded factors.

## 3.2 Important material and production fields are absent or incomplete

Cement type, cement source, and cement chemical or physical properties.

Fly-ash class/source, slag and other supplementary cementitious materials.

Chemical admixture product, type, and dosage; the existing admixture field is not sufficiently structured.

Aggregate source, size, gradation, absorption, specific gravity, and shape characteristics.

Reliable total/effective water calculation, including free moisture and all water adjustments.

Material costs and approved material-specific emission factors for cost or carbon objectives.

Mix-design revision/version and confirmation that the recorded batch is the approved design quantity.

## 3.3 The available batch records are sparse and heterogeneous

Only a minority of enterprise concrete tests contain usable batch information, and the complete modeling cohort is concentrated in a limited set of offices and suppliers. Combining different suppliers, plants, strength classes, specification ranges, and operational practices increases unexplained variation. A global model can therefore obscure useful local relationships.

## 3.4 Slump and air are downstream outcomes

Actual slump and air are measured after batching and transportation. They are affected by water addition, elapsed time, temperature, admixtures, truck mixing, and measurement conditions. They should be modeled as predicted constraints only when those upstream inputs are sufficiently recorded. The current slump model is weak, and the air model is moderate but still has a P90 error of about 2.2 percentage points.

## 3.5 Current candidate output is retrospective, not a new optimized design

The candidate-search script ranks historical test rows. It does not generate a validated new recipe. Repeated rows from mix 303425 show that this existing mix deserves closer analysis, but they do not establish how many pounds of cement can safely be removed. In addition, candidates from different required-strength classes and specifications should not be compared in one undifferentiated list.

# 4. What Would Be Needed to Improve ML-Based Optimization

| Need | Minimum improvement | Why it matters |
| --- | --- | --- |
| Structured materials | Cement/SCM/admixture product IDs, types, sources, dosages | Separates material chemistry and supplier effects |
| Water accounting | Batch water, free moisture, water added, effective water | Makes W/CM physically meaningful |
| Aggregate properties | Source, gradation, absorption, specific gravity | Explains water demand and strength variability |
| Design identity | Approved mix version and effective dates | Prevents combining materially different revisions |
| Objectives | Material costs and approved emission factors | Enables true cost/carbon optimization |
| Local coverage | Repeated complete records by plant and mix | Supports plant-specific validation |
| Validation | Out-of-time and held-out plant/office tests | Checks performance on future and unseen operations |
| Field trials | Engineer-approved trial batches after recommendation | Confirms safety before operational use |

Minimum gate for future optimization The strength surrogate should materially beat the Dummy baseline and maintain acceptable error on recent out-of-time data and held-out plants. Model quality alone is not enough; candidate recipes must also remain inside observed material ranges and pass engineering trial validation.

# 5. Recommended Next Step: Historical Mix Performance Analysis

Historical Mix Performance Analysis changes the question from “What new recipe should the model create?” to “Which existing mixes have demonstrated stable, specification-compliant performance and may deserve engineering review?” This approach relies mainly on actual test results and transparent statistics rather than a weak strength surrogate.

## 5.1 Unit of analysis

Create one summary row for each comparable mix group. The primary grouping should be:

Office → supplier → plant → mix number.

Required 28-day strength class.

Applicable slump and air specification ranges when available.

Mix-design revision/effective period if a reliable revision identifier can be obtained.

A recent analysis window (for example, the latest 18 months) plus an all-history reference.

Do not combine the same mix number across materially different suppliers, plants, required strengths, or specification ranges. Normalize aliases such as Duke City and Duke City Redi-Mix only after confirming they represent the same business/material source.

## 5.2 Required metrics for each group

| Category | Metrics | Purpose |
| --- | --- | --- |
| Coverage | Test count, date range, months with data | Shows whether evidence is sufficient and current |
| Strength | Mean, median, SD, coefficient of variation, P10, min/max | Measures level and variability |
| Compliance | Failure count/rate; tests below required strength | Measures demonstrated reliability |
| Margin | Mean/median/P10 strength margin | Finds consistent over-performance |
| Materials | Mean/median/range of cement, fly ash, total cementitious, W/C | Compares resource intensity |
| Fresh concrete | Slump/air sample count, mean, out-of-spec rate | Checks field performance |
| Consistency | Year/quarter trends and recent-vs-history shift | Detects deterioration or process changes |

## 5.3 Candidate rules

Use configurable, transparent rules rather than a single opaque score. A conservative first version can require all of the following:

Minimum number of valid 28-day tests (initial exploratory value: 30; materials engineer to approve).

No recent strength failures, or a failure rate below an engineer-approved limit.

P10 actual strength at or above required strength plus an approved buffer.

No evidence of recent downward trend or major increase in variability.

Adequate slump and air compliance coverage when those specifications apply.

Mean strength margin materially higher than comparable mixes in the same strength class.

Cement or total cementitious content higher than a stable peer mix, indicating possible review opportunity.

The output label should be “Engineering Review Candidate,” not “Reduce Cement” or “Optimized Mix.” The materials engineer decides whether additional design review or trial batching is appropriate.

## 5.4 Peer comparison

Compare a mix only with relevant peers: same required-strength class, similar applicable air/slump specification, and preferably the same regional market or supplier/plant. Useful peer measures include percentile rank of cement content, percentile rank of strength margin, failure rate, and P10 strength. This prevents an 8,000 psi mix from being compared directly with a 3,000 psi mix.

## 5.5 Recommended deliverables

mix_performance_summary.csv — one row per comparable mix group.

mix_review_candidates.csv — groups meeting the transparent review rules.

mix_data_quality_exceptions.csv — missing, inconsistent, and insufficient groups.

mix_test_detail.csv — underlying tests for engineer audit.

Executive summary charts — failure rate, P10 margin, cement use, and variability by mix.

# 6. Proposed Analysis Workflow

Validate identity fields. Standardize supplier/plant aliases carefully while preserving original values for audit.

Create comparable groups using office, supplier, plant, mix, required strength, and specification ranges.

Filter to standard-cured 28-day outcomes and valid US-unit batch quantities; retain exclusion reasons.

Calculate strength, failure, margin, material, field-compliance, and time-trend metrics.

Apply minimum sample-size and reliability gates before peer comparison.

Rank engineering review candidates within comparable peer groups; do not mix strength classes.

Export summary, candidate, exception, and underlying-detail files.

Review findings with a materials engineer, starting with recurring mix 303425 as a case study.

If a candidate is accepted for investigation, conduct a controlled design review and trial batch; do not change production quantities solely from IMTS analytics.

# 7. Pilot Case: Mix 303425

The candidate output repeatedly identified mix 303425 from Duke City-related suppliers/plants. Historical rows generally show approximately 407–419 lb/yd³ cement, 137–146 lb/yd³ fly ash, W/C around 0.41–0.45, a 3,000 psi required strength, and many actual 28-day results around 5,000–6,400 psi. This makes it an appropriate pilot for aggregation—not proof that cement should be reduced.

The pilot should separate Broadway, Duke City, and BW-1 plants; resolve supplier aliases; calculate recent and all-history performance; verify applicable air/slump specifications; and examine the full strength distribution. The key questions are whether the P10 strength and failure rate remain acceptable and whether the apparent margin is stable rather than driven by selected high results or an old mix revision.

# 8. Decision and Recommendation

Recommended path Proceed with Historical Mix Performance Analysis as the next IMTS analytics deliverable. Use the results to support, not replace, the professional judgment and approval process of a concrete/materials engineer.

| Use case | Current decision | Next action |
| --- | --- | --- |
| Automatic ML mix optimization | Do not proceed | Collect structured material data and revalidate locally |
| Automatic cement/carbon reduction | Do not proceed | Obtain emission factors/costs and require engineering trials |
| Historical mix performance analysis | Proceed | Build transparent group metrics and review rules |
| Mix-design review candidate list | Proceed with controls | Label as review-only and provide underlying test evidence |