# IMTS Mix Optimization Feasibility

Feasibility Assessment Using Available IMTS Batch and Day-0 Field Data

KEY RESULT: ExtraTrees produced the strongest results, but mean R² remained near 0.40 and errors were roughly 500–800 psi. The current IMTS data supports historical mix-performance screening and engineer review, but not fully automated mix-design optimization.

# Study design and validation

| Eligible dataset | 13,133 concrete test records with batch data that meet the mix-optimization analysis requirements. |
| --- | --- |
| Feature sets | 1) Batch data only; 2) Batch data + Day-0 field slump and air measurements. |
| Models compared | HistGradientBoosting, ExtraTrees, Random Forest, and DummyMedian. |
| Validation | 80% training / 20% held-out test split, with 5-fold project-grouped cross-validation used to evaluate model stability and performance. |
| Why DummyMedian? | A simple baseline that predicts the training-set median for every record. It shows whether the ML models add meaningful predictive value beyond a constant prediction. |

# Validated model performance

| Analysis | Best model | Records | Mean R² | R² range | MAE (psi) | RMSE (psi) |
| --- | --- | --- | --- | --- | --- | --- |
| Batch data only | ExtraTrees | 13,133 | 0.405 | 0.263–0.520 | 545 | 811 |
| Batch data + slump and air | ExtraTrees | 11,735 | 0.396 | 0.263–0.449 | 509 | 741 |

Interpretation: ExtraTrees performed best in both feature sets. Adding Day-0 slump and air reduced MAE from 545 to 509 psi and RMSE from 811 to 741 psi, but mean R² remained near 0.40, indicating only moderate predictive power for mix optimization.

# Why current IMTS data limits automated mix optimization

• IMTS purpose: IMTS was designed to record field placement conditions and scheduled strength-test results—especially 28-day strength—not to capture the full detail needed for mix-design optimization. • Batch-data coverage: More than 85% of concrete records do not contain batch data, which sharply reduces the amount of usable training data. • Data detail: The available batch records are not detailed or consistent enough to isolate how mix proportions and production variables drive strength with the reliability required for automated mix recommendations.

# Recommended Direction

BEST CURRENT USE Use 7-day and 28-day strength history to screen mix performance, identify recurring low-margin/failure patterns or consistent overstrength, and flag mixes for materials-engineer review. Machine learning should support the review—not automatically change a mix design. True optimization will require richer, standardized batch/mix-design data and validation through the approved trial-batch/submittal process.

# IMTS Concrete Predictive Quality Analysis

Summary of Regression, Risk Classification, and Model Comparison

Main finding: Day-7 information provides strong prediction of 28-day strength and strong quality-risk screening. The best results come from Day-7 data with Supplier, Plant, and Mix context.

# 1. Purpose

The goal of this analysis was to determine whether the current large IMTS concrete dataset can be used to predict concrete quality before the final 28-day strength result is available.

The analysis focused on two simple questions:

Can we predict the final 28-day concrete strength?

Can we identify concrete tests that may fall below the required 28-day strength?

The current IMTS concrete data was reviewed, and eligible records were used for modeling and validation. For the Day-7 analysis, 81,509 concrete samples from 4,107 projects were available.

# 2. Feature Sets

| Feature Set | Information Used | Business Meaning |
| --- | --- | --- |
| Day 0 - Field | Day-0 field measurements + required 28-day strength | Prediction when concrete is placed |
| Day 0 - Field + context | Day-0 field measurements + required 28-day strength + Supplier / Plant / Mix |  |
| Day 7 - Field | Day-0 field measurements + required 28-day strength + actual Day-7 strength information | Updated prediction after 7 days |
| Day 7 - Field + context | Day-0 field measurements + required 28-day strength + Day-7 strength + Supplier / Plant / Mix | Most complete prediction |

Models were validated using 5-fold project-grouped cross-validation. Tests from the same project were kept together, so the model was evaluated on projects that were not used to train that fold.

# 3. 28-Day Strength Prediction

Regression models answer the question: “What 28-day strength do we expect?” The output is a strength value in psi.

| Feature Set | Best Model | MAE | RMSE | R² |
| --- | --- | --- | --- | --- |
| Day 0 - Field | HistGradient Boosting | 699 psi | 955psi | 0.683 |
| Day 0 - Field + context | HistGradient Boosting | 663 psi | 918 psi | 0.707 |
| Day 7 - Field | XGBoost | 344 psi | 492 psi | 0.915 |
| Day 7 - Field + Context | HistGradient Boosting | 320 psi | 465 psi | 0.924 |

MAE (Mean Absolute Error): Average prediction error. Lower values mean predictions are closer to actual results.

RMSE (Root Mean Squared Error): Measures prediction error with extra emphasis on larger mistakes. Lower values are better.

R² (R-Squared): Indicates how well the model explains the data. Values closer to 1.0 indicate a better fit.

The Day-7 models were much stronger than the Day-0 model. The strongest result was Full Context + Day 7, with an average error of about 320 psi and R² of about 0.924.

# 4. Failure Risk Classification

Classification models answer a different question: “Is this test at risk of falling below the required 28-day strength?”

For this analysis, Failure = Actual 28-day strength < Required 28-day strength. This is an analytical risk flag, not the final engineering acceptance decision.

| Feature Set | Recall | Precision | F1 | FN | FP |
| --- | --- | --- | --- | --- | --- |
| Day 0 - Field | 60.9% | 12.9% | 0.212 | 1,901 | 20,055 |
| Day 0 - Field + Context(supplier, plant, mix ) | 63.0% | 14.3% | 0.233 | 1,801 | 18,401 |
| Day 7 - Field | 90.7% | 35.1% | 0.507 | 453 | 8,135 |
| Day 7 - Field + Context (supplier, plant, mix ) | 89.9% | 38.7% | 0.541 | 489 | 6,934 |

Positive class = Fail. A test is labeled Fail for this analytical screening when its actual 28-day strength is below the applicable required 28-day strength. Pass is the negative class.

Recall means: Of all tests that actually failed, what percentage did the model identify as Fail? For example, recall = 0.90 means the model found about 90% of the actual failures and missed about 10%.

Precision means: Of all tests the model flagged as Fail, what percentage were actually Fail?

The table above uses a classifier threshold of 0.50. Day 0 + Context is better than Day 0 Field alone, but Day-0 precision remains low. Day 7 is much stronger: the models identify about 90% of actual failures at the 0.50 threshold.

# 5. Regression-Derived Risk vs. Direct Classifier

A regression prediction can also be converted into a risk flag by comparing predicted 28-day strength with the required 28-day strength. I compared that approach with a separate classifier.

| Feature Set | Regression Recall | Regression Precision | Classifier Recall | Classifier Precision |
| --- | --- | --- | --- | --- |
| Day 0 - Field | 2.0% | 53.7% | 60.9% | 12.9% |
| Day 0 - Field + Context | 3.4% | 49.8% | 63.0% | 14.3% |
| Day 7 - Field | 49.4% | 66.7% | 90.7% | 35.1% |
| Day 7 - Field + Context | 51.5% | 68.4% | 89.9% | 38.7% |

At a strict regression margin of 0 psi, regression has higher precision but much lower recall. In other words, it creates fewer alerts, but it misses many actual failures. This is especially clear at Day 0 and still important at Day 7.

# 6. Precision-Recall trade-off for the Direct Classifier

Each point on the curve represents a different classification threshold

This plot shows the trade-off between recall and precision as we change the classification threshold. As recall increases, precision decreases because the model generates more false alarms. The Day 7 models perform significantly better than the Day 0 models, and Full Context plus Day 7 generally provides the best precision at the same recall level.

# 7. Main Findings

| Question | Finding |
| --- | --- |
| Can IMTS predict 28-day strength at Day 0? | Partially. Accuracy is limited. |
| Can IMTS predict 28-day strength at Day 7? | Yes. Strong performance. |
| Does Supplier / Plant / Mix information help? | Yes, moderately. |
| Can IMTS identify tests at risk of falling below required strength? | Yes, especially after Day 7. |
| Does a separate classifier add value? | Yes. It finds failures more efficiently at similar recall. |
| Is Day 0 ready for strong operational alerts? | No. Better as preliminary screening. |
| Is Day 7 suitable for predictive quality screening? | Yes. This is the strongest current use case. |

# 8. Recommended Direction

The strongest current use case is:

Day-7 Updated Concrete Quality Risk Screening

A user could see both the strength prediction and the risk result together:

| Day-7 Quality Prediction | Example Result |
| --- | --- |
| Required 28-Day Strength | 4,000 psi |
| Predicted 28-Day Strength | 4,480 psi |
| Predicted Margin | +480 psi |
| Quality Risk | Elevated |
| Model Stage | Day 7 |

The regression model answers: “What strength do we expect?” The classification model answers: “How concerned should we be that this test may fall below the required strength?” These questions are related, but they are not exactly the same.

# 9. Overall Conclusion

The current large IMTS concrete dataset provides strong predictive value after the 7-day strength result becomes available. Project-grouped cross-validation showed that the Day-7 regression models can predict 28-day strength with an average error of approximately 320–345 psi and R² above 0.91.

The Day-7 classification models also showed strong ability to identify concrete tests that may fall below the required 28-day strength. When regression-based and classification-based risk methods were compared at similar recall levels, the direct classifier consistently produced fewer false alerts.

The results support using both predicted 28-day strength and a separate quality-risk score in a Day-7 predictive quality screening tool. Day-0 predictions may still provide early information, but they are not currently strong enough for reliable failure-risk alerts.